Bath-1: SPM

Operating: 110 – 150, H2SO4/ H2o2 (3:1), Circulation

Chemical spiking: auto concentration feedback

Bath Materials: Quartz

Bath-2 QDR (hot)

Operating: DIW rinse (75 degrees Celsius. 40-80 L/min)

Injection: H202/NHOH

Bath Materials: PTFE

Megasonic: 950 kHz, 2400W (600*4)

Bath-3: APM

Operating 35-85 degrees Celsius/ NH4OH/DIW (1:1:15), 15 L/min, circulation

Chemical spiking : Auto concentration feedback

Bath Materials: PTFE

Megasonic: 950 kHz, 24000W (600*4)

Bath-4 POU

Operating: 70 degrees Celcius. NH4OH/H2O2

DIW Shower (hot/cold)

Bath Materials: PTFE

Megasonic: 950 kHz, 2400W (600*4)

Dryer: SD2*2

Operating: 49% DHF (1:200), IPA/N2 200 degrees Celsius , 100 L/min

Resistivity monitoring (Horiba)

Bath Material: PTFE

Damaged / missing parts: none reported.